Custom Sample Process

Step 1.

Terrazzo can be manufactured to produce flooring and surfaces with various designs, looks, and applications. Selecting and working with different aggregate materials, colors, and adhesives means there is much thought and planning that goes into the sample making process.

The first step is having a color or mood in mind for the resin or adhesive that will be used to bond with the terrazzo aggregate. This establishes the base color the floor or surface will take.

The next step is deciding what type and color aggregate to use with the chosen adhesive color. Example aggregate types include: marble, quartz, granite, recycled glass, recycled porcelain, recycled concrete, and various metals.

Terrazzo Masters has a wide range of terrazzo color pallets and samples to choose from in case you can’t decide on a specific color or aggregate.

Step 2.

Now that you have the ideal materials chosen for your sample, the next step is deciding on the size of the aggregate mix.

Aggregate sizes range from fine to large aggregate on a scale system from #00 to #8.

The standard terrazzo aggregate sizes are usually #0, 1, 2. Aggregate size #00 is considered more of a premium terrazzo, while #3 – #8 terrazzo is classified as venetian style terrazzo and is also considered premium.

Step 3

Now that the color and sizes of the terrazzo has been chosen, it is now time to develop the blend of terrazzo. The blend is based on a total aggregate mix of 100% that combines different percentages of aggregate to form the final 100% blend.  The lowest percentage of aggregate should not be less than 5%.

Additionally, while considering the overall terrazzo blend, we will need to specify the grit and sealer used in the terrazzo. Most projects use a 200 grit finish and WB Acrylic Sealer for cost effectiveness, but other options exist such as WB Urethane Sealer.

Step 4

We suggest ordering multiple samples to help you decide which sample mix would be best for your project. Sometimes the sample won’t be what you had in mind or visualized.

Samples will take ~2 weeks to properly develop before being shipped out.

It is recommended to set the sample on the ground and look down at it to best visualize how it will look across the surface.

If you have any questions about creating your terrazzo sample, please get in touch with Terrazzo Masters, where we will try and answer any questions you may have regarding the sample.

Once a sample has been selected, contact Terrazzo Masters to proceed with your commercial flooring or surfacing project.